European Union Risk Assessment Report

Voluntary Risk assessment of COPPER, COPPER II SULPHATE PENTAHYDRATE, COPPER(I)OXIDE, COPPER(II)OXIDE, DICOPPER CHLORIDE TRIHYDROXIDE

CAS No: 7440-50-8, 7758-98-7, 1317-3-1, 1317–38–0, 1332-65-6

EINECS No: 231–159–6, 231–847–6, 215-270-7, 215–269–1, 215-572-9

Responsible for this voluntary risk assessment : European Copper Institute (ECI)

Contact person: Dr. Katrien Delbeke, European Copper Institute, Brussels, Belgium

e-mail: kmd @eurocopper.org

Review country for this voluntary  risk assessment : Italy

Contact person: Dr. Roberto Binetti , Istituto Superiore di Sanità, Rome, Italy

e-mail: binetti@iss.it

CHAPTER 3 – Environmental Hazard classification

Appendix K2: Hazard Classification of Massive Copper Forms

Patricio H. Rodriguez, Katrien Delbeke and William Adams

Lead author : P. Rodriguez, Centro de Investigacion Minera y Metalurgica (CIMM), e-mail : prodrigu@cimm.cl

| Date of Last Literature Search : | 2004 |
| --- | --- |
| Review of report by MS Technical Experts finalised: | April 2008 |
| Final report: | June 2008 |

LEGAL NOTICE

Neither the European Commission nor any person acting on behalf of the Commission is responsible for the use which migh be made of the following information

A great deal of additional information on the European Union is available on the Internet.

It can be accessed through the Europa Server(http://europa.eu.int).

Foreword

In response to a request from the European Commission to “start preparing the initial assessments for substances on the EU working list as these were considered as Community priorities in the context of the industry voluntary initiatives for high production volume chemicals” the copper industry committed to undertake a Voluntary Risk Assessment (VRA) for copper and the copper compounds on the EU working list: Cu, CuO, Cu2O, CuSO4 and Cu2Cl(OH)3. This initiative was endorsed by the EU CAs in 2001. Yearly summaries on progress have been presented at the CA meeting.

This comprehensive VRA dossier has taken four years to complete, with the whole process managed by the European Copper Institute. It was compiled in co-operation with expert consultants from the University of Birmingham/ICON for human health toxicity, from BR. Stern and Associates for human health deficiency, and from Euras/Ecolas for the environment. It is based on the principles of Regulation 793/93, 1488/94 and the detailed methodology laid down in the revised Technical Guidance Document on Risk Assessment for New and Existing Substances. Methodological experiences gained through other metal Risk Assessments, e.g. the incorporation of bioavailability for zinc, were incorporated as appropriate. Additional up to date scientific information was integrated into the assessment where scientifically relevant (i.e. the use of bioavailability models for water, sediment and soil, plus information on copper as an essential nutrient). A broad cross section of the European copper industry has been fully involved in the process and has submitted a significant amount of proprietary data.

To ensure the transparency and quality of the dossier, the initial draft RA reports have been refined by incorporating inputs from the Review Country (Italy – Istituto Superiori di Sanità) and independent peer review panels.

For several of the substances under consideration, targeted risk assessments are required under the Biocidal Product Directive (98/8/EC) and the Plant Protection Products Directive (91/414). These dossiers, which have been/will be provided to the competent authorities (France) by the respective end user industry groups, contain confidential information not available to ECI. However, ECI has worked closely with both of these groups in incorporating relevant information to ensure consistency to the extent possible.

A single dossier covers the assessments for copper metal and the copper compounds, with substance specific aspects provided where relevant. For the base data compilation, extensive literature searches were performed for each substance. Data gaps were filled with analogous data, where relevant, or by additional testing where possible. Where the information was either unnecessary for the copper risk assessment, or impossible to obtain, waiving for testing and/or justification to support derogation is discussed. Some remaining data gaps were identified and will be tackled as a follow-up to this report.

Since the initial submission of the dossier on 15 May 2005, comments have been received from several Member States. The current version reflects comments made by the Member States in writing and during the TCNES meetings. To ensure the transparency and quality of the dossier, the current version and the responses to Member States comments have been refined in close co-oporation with the Review Country (Italy – Istituto Superiori di Sanità).

The human health and environmental sections of the report have been agreed by TCNES (see TCNES opinions) and sent to SCHER for final review.

This Draft Risk Assessment Report is the responsibility of the European Copper Insitute (ECI).  The member companies of the copper industry risk assessment consortium are the owners of the assessment.  These companies are listed below.

Industries/companies wishing to use all or part of the Risk Assessment Reports, and/or their appendices, for regulatory purposes such as for EU REACH registrations, EU Biocidal Products Directive Registrations, or EU Plant Protection Product Directive Registrations, are required to contact ECI to agree terms of access.

In order to avoid possible misinterpretations or misuse of the findings in this draft, anyone wishing to cite or quote any part of this report, or its related appendices, is advised to contact ECI beforehand.

Contact details of the responsible:

Dr. Katrien Delbeke, European Copper Insitute, Tervurenlaan 168, B-1150 Brussels, Belgium.  Tel: +32 2 777 7083, e-mail: kmd @eurocopper.org

Ownership

The industry companies that are part of the industry consortium are listed here:

|  | COPPER VOLUNTARY RISK ASSESSMENT - COMPANY MEMBERS IN INDUSTRY CONSORTIUM |  |
| --- | --- | --- |
| SITE | ADDRESS | CITY | COUNTRY |
| ALCHEMA | East Ord Industrial Estate | Berwick Upon Tweed TD15 2XF | UK |
| ANGLO AMERICAN BASE METALS | 20 Carlton House Terrace | London SW1Y 5AN | UK |
| ANTOFAGASTA MINERALS S.A. | Ahumada 11 - Piso 6 | Santiago | CHILE |
| Atlantic Copper - Cordoba | Barriada Electromecanica, s/n | E-14005 CORDOBA | SPAIN |
| Atlantic Copper Barcelona | Ctra. Palaudaries, Km 0.4 | E-08185 Llica de Vall | SPAIN |
| ATLANTIC COPPER HOLDING S.A. -Huelva | Avda Francisco Montenegro, s/n | E-21001 HUELVA | SPAIN |
| B. MASON & SONS LTD. | WHARF STREET, ASTON | BIRMINGHAM B6 5SA | UK |
| BHP Billiton Plc | Avenida Americo Sur Nr. 100 - 8th Floor | Santiago | CHILE |
| BOLIDEN AB. | Smaltverket | S-93281 Skelleftehamm | SWEDEN |
| BOLIDEN CUIVRE ET ZINC | RUE DU FOURNEAU, 43 | B-4030 GRIVEGNEE (LIEGE) | BELGIUM |
| BOLIDEN LDM NEDERLAND B.V. | P.O. BOX 42 - LIPSSTRAAT 44 | NL-5150 AA DRUNEN | NETHERLANDS |
| BOLIDEN MINERAL AB | Klarabergsviadukten 90 | SE - 101 20 Stockholm | SWEDEN |
| BRAZE TEC GmbH | Rodenbacher Chaussee 4 | D-63457 Hanau-Wolfgang | GERMANY |
| BUNTMETALL AMSTETTEN GES.M.B.H. | FABRIKSTRASSE 4 | A-3300 AMSTETTEN | AUSTRIA |
| CODELCO-Chile | Huerfanos 1270, piso 11 | 650-0544 Santiago | CHILE |
| Compañia Minera Doña Ines Collahuasi | Av. Andres Bello 2687 Piso 11 | Las Condes, Santiago 6760276 | CHILE |
| Compañia Mineraria Zaldívar | 1125 Seventeenth Street, Suite 2310 | Denver, Colorado 80202 | USA |
| CUMERIO (was Umicore Copper) | Watertorenstraat 33 | B-2250 OLEN | BELGIUM |
| DEUTSCHE GIESSDRAHT GmbH | Kupferstraße 5 | D-46446 EMMERICH | GERMANY |
| ELMET S.L. | Barrio Arene 20 | E-48640 BERANGO (Vizcaya) | SPAIN |
| ENZESFELD-CARO METALLWERKE AG | Postfach 1, FABRIKSTRASSE 2 | A-2551 ENZESFELD/TRIESTING | AUSTRIA |
| Erachem Comilog SA | Rue du Bois | B-7334 Saint-Ghislain | BELGIUM |
| EUROPA METALLI S.P.A Fornaci | Via della Repubblica, 257 | I-55052 Fornaci di Barga (Lucca) | ITALY |
| EUROPA METALLI S.P.A. Serravalle | Via Cassano 113 | I-15069 Serravalle Scrivia (Alessaandria) | ITALY |
| EUROPA METALLI SpA Campo Tizzoro | Viale L. Orlando 325 | I-51023 Campo Tizzoro (Pistoia) | ITALY |
| HALCOR METAL WORKS S.A. | 16 Himaras Str. | Maroussi , GR 151 25 | GREECE |
| HALCOR METAL WORKS S.A. casting shapes | Foundry, Oinofyta (55th km) | GR | GREECE |
| HALCOR METAL WORKS S.A. rolling mill | Rolling Mill, 252 PIRAEUS STREET | GR-17778 ATHENS | GREECE |
| HALCOR METAL WORKS S.A. tube | Copper Tube Mill, Oinofyta (57th km) | GR | GREECE |
| HÜTTENWERKE KAYSER AG. | Postfach 15 60, Kupferstraße 23 | D-44505 LÜNEN | GERMANY |
| IBP Group Services Limited | Whitehall Road | Tipton, West Midland DY4 7JU | UK |
| ISAGRO (ex Caffaro) | Via Caldera, 21 | 20153 Milano | ITALY |
| KGHM Polska Miedz SA | ul. Sklodowsklej-Curie 48 | 59-301 Lubin | POLAND |
| KM EUROPA METAL AG | POSTFACH 3320, Klosterstraße 29 | D-49023 OSNABRUECK | GERMANY |
| KME - Berlin | Miraustraße 10-14 | D-13509 Berlin | GERMANY |
| KME - Menden | Carl-Benz-Straße 13 | D-58706 Menden | GERMANY |
| KME Group | P.O. Box 33 20 Klosterstrasse | D-49074 Osnabruck | GERMANY |
| LA FARGA LACAMBRA, SA | Ctra C-17, Km 73,5 COLONIA LACAMBRA | E-08509 LES MASIES DE VOLTREGA (BARCELONA) | SPAIN |
| MANICA | Via all'Adige,4 | 38068 ROVERETO (Trento) | ITALY |
| Méxicana de Cobre, S.A. de C.V. | Baja California No. 200 Sixth Floor | Mexico City 06760 | MEXICO D.F. |
| Minera Escondida Limitada | Avenida Americo Vespucio Sur Nr. 100 - 9th Floor | La Condes, Santiago | CHILE |
| Mitsubishi Materials Corporation | 20F OtemachiFirst Square West, 1-5-1, Ohtemachi, Chiyoda-KU | 100-8117 Tokyo | JAPAN |
| MKM MANSFELDER KUPFER UND MESSING GMBH | POSTFACH 1254, Lichtlöcherberg 40 | D-06323 HETTSTEDT, D-0ß6333 Hettstedt | GERMANY |
| MUELLER INDUSTRIES, Inc. | 8285 Tournament Drive, Suite 150 | Memphis, TN 38125 | USA |
| NEXANS | 4-10, rue Mozart | 92587 Clichy Cedex | FRANCE |
| NEXANS BOURG EN BRESSE | PO Box 101 | F-01003 Bourg en Bresse | FRANCE |
| Nexans IKO Sweden AB |  | S-514 81 Grimsas | SWEDEN |
| NEXANS MEHUN SUR YEVRE |  | F-18500 Mehun Sur Yevre | FRANCE |
| NEXANS WIRES CHAUNY | 128, avenue Jean Jaures, BP30 | F-02301 Chauny | FRANCE |
| NEXANS WIRES MÂCON | Rue du Port | F-71000 Macon | FRANCE |
| Nippon Mining & Metals Co., Ltd | Toranomon 2-chome, Minato, Ku | 105-0001 Tokyo | JAPAN |
| NORANDA Inc. | Avda Andrés Bello 2777 Oficina 801 | Las Condes, Santiago 6760276 | CHILE |
| NORDDEUTSCHE AFFINERIE AG. | Postfach 10 48 40, Hovestraße 50 | D-20033 HAMBURG, D-20539 Hamburg | GERMANY |
| NORDIC BRASS AB | Box 524 | S-721 09 Västeras | SWEDEN |
| Nordox Industries AS | Ostensjovn. 13, PB 6639 Etterstad | N-0607 Oslo | NORWAY |
| OK Tedi Mining Limited | P.O. Box 1, Dakon Road, Tabubil | Western Province, Papua | NEW GUINEA |
| OMG Kokkola Chemicals Oy | PO Box 286 | 67101 Kokkola | Finland |
| OUTOKUMPU American Brass | 70 Sayre Street, P.O. Box 981 | Buffalo, NY 14240 | USA |
| OUTOKUMPU COPPER Products AB | Box 510, Metallverksgatan 5 | S-721 88 VAESTERAS, S-721 09 Västeras | SWEDEN |
| OUTOKUMPU Copper Products Oyj | Riihitontuntie 7 A, P.O. Box 144 | Espoo FIN-02201 | FINLAND |
| OUTOKUMPU COPPER STRIP AB | Metallverksgatan 20-22 | S-721 88 VAESTERAS, S-721 10 Västeras | SWEDEN |
| Outokumpu Copper Strip AB- Finspang |  | S-612 81 Finspang | SWEDEN |
| OUTOKUMPU COPPER TUBES S.A. | Bº ARKOTXA S/N | E-48480 ZARATAMO | SPAIN |
| OUTOKUMPU HARJAVALTA METALS OY | P.O.Box 89 | FIN-29200 Harjavalta | FINLAND |
| OUTOKUMPU MKM LTD. (ex Boliden MKM) | MIDDLEMORE LANE - ALDRIDGE | WALSALL, West Midlands WS9 8DN | UK |
| Outokumpu Nordic Brass AB (was BOLIDEN GUSUM AB) | Gräsdalens Industrial site | S-610 40 GUSUM | SWEDEN |
| OUTOKUMPU PORICOPPER OY | P.O. Box 60 | FIN-28101 Pori | FINLAND |
| P.T. Freeport Indonesia Inc. | 1615 Poydras Street P.O. Box 51777 | New Orleans, Louisiana 70112 | USA |
| PALABORA Mining Company | P.O. Box 65 Phalaborwa, 1390 | Limpopo Province | SOUTH AFRICA |
| Phelps Dodge Corporation | One North Central Avenue | Phoenix, AZ 85004 | USA |
| PRYMETALL GMBH & CO. KG | Zweifaller Strasse 150 | D-52224 Stolberg | GERMANY |
| Revere Copper Products Inc. | One Revere Park | Rome, NY 13440-5561 | USA |
| RIO TINTO Plc | 6 St. James' Square | London SW1Y 4LD | UK |
| Sahna Kaimer GmbH/KG | Im Teelbruch 80 | D-45219 Essen-Kettwig | GERMANY |
| SCHWERMETALL HALBZEUGWERK GMBH | POSTFACH 6264, Breiniger Berg 165 | D-52211 STOLBERG, D-52223 STOLBERG | GERMANY |
| SOCIETE DE COULEE CONTINUE DE CUIVRE | 42 RUE FERDINAND-BUISSON - B.P. 105 | F-02301 CHAUNY CEDEX | FRANCE |
| SOCIETE LENSOISE DU CUIVRE | Boulevard du Marais | F-62300 LENS CEDEX | FRANCE |
| SPIESS URANIA | Heidenkampsweg 77 | D-20097 Hamburg | GERMANY |
| STOLBERGER METALLWERKE GMBH & CO. KG | POSTFACH 1929, Frankentalstraße 5 | D-52206 STOLBERG, D-52222 Stolberg | GERMANY |
| SUMITOMO Metal Mining Co., Ltd | 1 1-3, Shimbasi 5-Chome, Minato-KU | 105-871 6 Tokyo | JAPAN |
| Thyssen Krupp VDM | Plettenberger Strsse 2 | D-58791 Werdohl | GERMANY |
| TREFILERIES ET LAMINOIRS DE LA MEDITERRANEE | 35 RUE LE CHATELIER | F-13015 MARSEILLE CEDEX 15 | FRANCE |
| TREFIMETAUX - Givet Plant | Rue des Vieilles Forges | F-08600 Fromelennes | FRANCE |
| TREFIMETAUX - Niederbruck | 31, Rue Joseph Vogt | F-68290 Niederbruck | FRANCE |
| TREFIMETAUX - Serifontaine | Rue M. Thorez, BP3 | F-60590 Serifontaine | FRANCE |
| TREFIMETAUX --usine de Boisthorel |  | F-61270 Rai | FRANCE |
| UMICORE ITALIA SRL | nucleo industriale di Pianodardine (Avellino) | I-AVELLINO | ITALY |
| WEDNESBURY TUBE & FITTINGS - MUELLER EUROPE | OXFORD STREET | GB- BILSTON WEST MIDLANDS WV14 7DS | UK |
| WIELAND-WERKE AG Ulm Vöhringen | POSTFACH 42 40, Graf-Arco-Straße 36 | D-89070 ULM, D-89079 ULM | GERMANY |
| WIELAND-WERKE AG, WERK LANGENBERG | POSTFACH 110269, Ziegeleiweg 20 | D-42530 VELBERT, D-42555 VELBERT | GERMANY |
| WIELAND-WERKE AG, WERK VILLINGEN | POSTFACH 1780, Lantwattenstr 11 | D-78007 VILLINGEN, D-78050 VILLINGEN-SCHWENNINGEN | GERMANY |
| WILLIAM BLYTHE LIMITED | Church, Accrington | Lancashire, BB5 4PD | UK |
| WMC Copper uranium/WMC Resources Limited | IBM Tower 60 City Road | Southbank Vic 3006 | AUSTRALIA |
| Wolstenholme International | Springfield House, Lower Ecclesfield Road, Darwen | Lancashire BB3 0RP | UK |
| XSTRATA Copper | Level 9, Riverside Centre, 123 Eagle Street | Brisbane Q 4000 | AUSTRALIA |
| YORKSHIRE COPPER TUBE LTD. (KME) | East Lancashire Road, Kirby | LIVERPOOL L33 7TU | UK |
| YORKSHIRE Fittings Ltd | P.O. Box 166 | Leeds, LS10 1NA | UK |
| European Copper Institute - May 12th 2005 |  |  |  |

COPPER, COPPER II SULPHATE PENTAHYDRATE, COPPER(I)OXIDE, COPPER(II)OXIDE, DICOPPER CHLORIDE TRIHYDROXIDE

CAS No: 7440-50-8, 7758-98-7, 1317-3-1, 1317–38–0, 1332-65-6

EINECS No: 231–159–6, 231–847–6, 215-270-7, 215–269–1, 215-572-9

VOLUNTARY Risk Assessment

Appendix K2:   Hazard Classification of Massive Copper Forms

Patricio H. Rodriguez1, Katrien Delbeke2 and William Adams3

1Centro de Investigacion Minera y Metalurgica (CIMM)

2European Copper Institute

3Rio Tinto

Introduction

The goal of this report is to propose a classification for the massive forms of metallic copper. The experimental design follows the recommendations of the OECD guidance document on transformation/dissolution (T/D) (OECD 2001) and the standard operating procedures (SOP) proposed by CANMET and LISEC for the Dissolution Transformation protocol to the ad hoc OECD Validation Management Group (VMG).  It is recognized from past work that key parameters in the test design are surface area, pH, loading and stirring rate (presented in order of importance).  These variables were evaluated and accounted for in the overall conclusions.  Tests were performed at loadings of 1 and 100 mg/L for 7 days and 1 mg/L for 28 days.  Data in this report focus on a pH of 6 since it is recognized that at this pH copper will deliver more soluble metal in solution than either pH 7 or 8.  A pH of 5.5 was not evaluated as test methods are not standardized or validated to accommodate this pH.  Additionally, copper dissolution is sensitive to the amount of CO2 used and maintaining a pH of 5.5 would require increased levels of CO2.

Experimental design

All the experiments presented in this report were carried out at CIMM (Centre for Mining and Metallurgy Research) in Chile. The dissolution transformation assays presented here were performed following closely the SOP prepared by CANMET and LISEC for the OECD VMG The Standard Operating Procedure for the Transformation/Dissolution of Metals and Sparingly Soluble Metal Compounds, Version February 2004.

Experimental design in summary

Samples of commercially available industrial copper wires type ETP 110 (Electrolytic Tough-Pitch) were used in all assays. The advantage of using copper wires is their very precise and reproducible geometry, which allows for precise calculation of exposed surface. Different wire diameters were used in order to control the amount of exposed surface at a given loading.

For the acute classification, the assays were performed over 7 days, at 1 and 100 mg/L loading in modified media OECD 203 (ISO 6341) diluted 10 fold and buffered to pH 6.0 with CO2 0.5%. The chronic assay was performed in the same type of media at 1 mg/L loading for 28 days.  Measurements of dissolved copper were carried out in a Class 1000 clean room using an ICP-MS instrument.

The samples were agitated in an orbital shaker. The stirring rate was controlled in each experiment. The details of the SOP are described in some detail in the Annex II.

Results

1.- Optimization of the stirring rate:

In the case of massive copper, the stirring rate seems to be a major factor for the release of copper ions into solution. Annex 9 of the GHS states: United Nations. 2003. The Globally Harmonized System of Classification and Labelling of Chemicals. Annex 9. pp 437.

“A 9.5.1.9 during the full transformation/dissolution tests, agitation should be used which is sufficient to maintain the flow of aqueous medium over the test substance while maintaining the integrity of the surface of the test substance and of any solid reaction product coatings formed during the test.”

Preliminary experiments indicated that stirring rate could be an important issue for copper dissolution.  It is thought that the formation of the oxide coating on the copper surface could be abraded under vigorous stirring action.  To evaluate the potential for effects from stirring we measured dissolved copper at different stirring rates (RPM). The assay was performed for 24 h at agitation rates going from rest to 100 rpm. The results are shown in Figure 1.

Figure 1. Dissolution transformation (0.16 mm diameter) at pH 6.0, 100 mg/L loading for 24 hours of copper wire.

With no stirring, there is a release of copper of 11 µg/L. This represents free diffusion across metal oxide and aqueous boundary layers resulting in a steady state concentration.  In previous studies carried in our Lab, we had demonstrated that a fully soluble substance, like CuSO4 x 5H2O, at rest is able to reach full solubility and homogeneity in less that 20 minutes, and at 50 RPM in less that 30 seconds. The increase in the concentration of dissolved copper to 45 ug/L at 100 RPM can be explained by the abrasion of the surface oxide coating of the metal as the metal is oxidized. The formation of a very labile thin film of corrosion product has been previously observed by Feng et al.(1996) Feng et al (1996), Corros. Sci. 38, pp .387-395 who discuss this phenomenon in detail. Using this supporting information, and in keeping with the intent of the GHS Annex 9, we chose to perform the dissolution transformation assays at 50 RPM. The choice of 50 RPMs is based on the shape of the curve.  It can be observed that little change in dissolution occurred in the 20-40 RPM range.  At 50RPMs and above a rapid increase in dissolution occurs as a function of the abrasion of the copper oxide layer.  Considering that preliminary experiments showed complete dissolution of a soluble salt in 30 seconds at 50 RPMs, this rate seems more than adequate to insure homogeneity of the aqueous test media.

2.- Validation of the principle of surface loading for copper massive.

In performing these experiments we choose to demonstrate the T/D of copper massive based on examination of surface area and the critical surface concept.  This approach is recognized in the GHS Classification system, Annex 8. The rational is based on the concept that the surface of the particles is in contact with the assay solution and most of the substance within the core of the particle is not in contact with the dissolution media, hence surface area is a critical parameter to assess. This is particularly critical in the case of the classification of massives, where the protocol allows for a default particle size of 1mm in diameter. These issues were discussed by Skeaff et al Skeaff, J.; Delbeke, K.; Van Assche F, and Conard, B. (2000) Environmental Toxicology and Chemistry. 19, pp. 1681-1691., who proposed a functional linkage between mass loading, surface loading and the ecotoxicological cut off values. To demonstrate that the classification of copper massives we believe it is necessary to follow this scheme.  Thus, we compared the results of the time course of the dissolution transformation of two wires with different geometries (0.16 mm and 0.4 mm diameter) at pH 6.0 for 28 days.  Wires were chosen for several reasons: (1) they are commercially available (2) wires of different diameters are available, (3) the diameter of each wire is precisely known thereby allowing for an exact calculation of the surface area based on length and diameter, (4) the chemical  purity of copper wires is very high (>99.9% copper) and (5) the surface area of a 1 mm particle (spherical in shape) is easily related to an equivalent piece of wire thereby allowing one to estimate how much wire should be tested to be equivalent in surface area to a 1 mm spherical particle.

In the first assay shown in figure 2, surface loading was kept constant at 1.22 mm2/L and the mass loading for the 0.16 mm and 0.4 mm wires was 0.43 mg/L and 1 mg/L, respectively. The dissolved amount of copper released by the 0.16 mm and 0.4 wires was 5.4 ug/L and 5.2 ug/L, respectively. These results clearly demonstrate that at same surface loading the release of the metal is the same and supports the view that massives should be classified using as main parameter the exposed surface loading.

In setting up experiments to evaluate massive T/D one has to choose between holding the loading constant, say 1 mg/L as recommended in the T/D protocol, or keeping the surface area constant.  It is not possible to do both in a given experiment.  When the surface is constant, the loading must increase in the test vessel with the largest mass.  In the present experiment, we minimized this by our choice of wires such that with constant surface area the loadings were at 0.43 and 1 mg/L.  Thus, both were close to the desired loading of 1 mg/L.  We believe this is the most appropriate way to perform the experiment.

Figure 2.- Effect of the exposed surface loading on the onset of the release of copper from copper wires. Constant surface loading of 1.22 mm2/L and mass loading 0.43 mg/L and 1 mg/L for the 0.16 mm and 0.40 mm wires respectively

Elaborating on this approach, Figure 3 shows the relationship between surface area loading and dissolved copper concentration after 7 days of transformation/dissolution at pH 6. Four types of copper wires were tested, using large variations in mass- loadings (1 & 100 mg/L)  and surface loadings (from 1.22 to 281 mm2/L). The detailed test set-up and results can be seen from Annex 1. These data clearly show (R2 = 0.98) the dependence of dissolution of massive copper on the surface area of the material tested.

Figure 3.- Linear relationship of dissolved released copper at pH 6.0 for 7 days and the surface loading.

In contrast, if one were to plot dissolution as a function of loading, the relationship would be curvilinear indicating that loading by itself cannot account for dissolution.  That is, one can keep the loading (mass) constant and achieve different amounts of metal in solution if the surface areas are different.  This is critical to understanding the dissolution of massive metals.

3.- Methodology used for the classification of copper massives

Since the GHS agreed  United Nations. 2003. The Globally Harmonized System of Classification and Labelling of Chemicals. Annex 8, pp 394. ST/SG/AC.10/30 on a default value of 1 mm particles for the massive classification we have devised a method in which the 1 mm particles is represented by a sphere of 1 mm in diameter. Problems frequently encountered assessing massives are centered around particle selection, surface area measurement and representativeness of the particles. The current approach avoids issues associated with the selection of a given particle type or preparation of particles specifically for classification purposes (non-commercial particles) and avoids the need for measuring the surface area as it can be precisely calculated.

Considering the relation between the surface loading and the release of copper, we thus determined the amount of metal released per surface unit (µg Cu/mm2) after 7 (28) days of transformation/dissolution and normalized these values to the amount released by the surface of a sphere of 1 mm in diameter at the cut-off  mass loadings of 1,10 and 100 mg/L.

Procedure

In general for Massive Substances

The mass of a metal sphere of 1 mm in diameter (Msph) corresponds to the volume of the sphere (Vsph) times the substance density (D).

Msph (mg) = Vsph (mm3)* D (mg/mm3)         (Eq. 1)

where Vsph = 0.5436 mm3 for a 1 mm sphere

Vcv is defined as the necessary volume of solution at the cut off value (CP) that contains Msph:

Vcv (L) = Msph (mg) / CP         (Eq. 2)

The Normalized Critical Surface Loading (mm2/L) at each cut off value is defined as:

NCSL (mm2/L) = SAsph / Vcv (L)      (Eq. 3)

Where SAsph is the surface area of a sphere 1 mm in diameter :

SAsph = 3.1416 mm2

For each of the standard cut off values (CP) the normalized critical surface loading (NCSL) becomes equal to:

NCSL (mm2/L) = 3.1416 mm2 * CP (1, 10, 100 mg/L) / [0.5236 mm3 * D (mg/mm3)]  (Eq. 4)

Now the NCSL of each standard cut off values can be used to calculate the amount of copper released at the end point of the dissolution transformation assay. This is necessary to determine the amount of dissolved substance released by mm2 at the end point of the assay at a any given mass loading (the substance specific surface area, in mm2/mg, is required). This method assumes that the release of metals ions to the solution is directly related to the surface loading, which has a strong fundamental basis.

For example for copper with a density is 8.9 mg/cm3,  at a cut-off loading of 1 mg/L , the NCSL corresponds to 0.67 mm2/L

Now, having the amount of dissolved substance release per surface unit (as µg/mm2)  at the end point (7 days for acute and 28 days for chronic classification) from the T/D assay, the value is then normalized to the surface loading of a sphere of 1 mm in diameter. This is necessary to calculate the NCSL for each cut off value and calculate the amount released at each NCSL

For example, if at a loading of 1 mg/L a given substance releases the amount of X1 ug/mm2, then normalized concentration values for the substance (NCV) released per NCSL is equal to:

NCV 1mg/L = NCSL 1mg/L (mm2/L) * X1 µg/mm2 ( where NCV is expressed in µg/L)

The calculated Normalized Concentration Values expressed in µg/L (a value which relates to a given surface area) can now be used to classify the substance by comparison to the L(E)50 ecotoxicological value.

4.- Acute Hazard classification of copper massives

T/D studies were performed at a pH of 6, 7 and 8.  All data are presented in Figure 4 and detailed results can be seen from Annex I.

Figure 4.  Comparison of dissolved released copper after 7 days of transformation dissolution  of different copper surface loadings at pH 6, 7 and 8.

The data show that the copper concentrations released at pH 7 & 8 are 5 to 10 times lower than the copper concentrations releasesd at pH 6.

The resulting data are summarized below and presented in detail in Annex I.

A copper species mean measured L(E)C50 value of 29 µg Cu/L  (27 µg Cu/L based on BLM normalized data) was used for the acute hazard classification. This value is the acute  ecotoxicty reference value representative for pH 6 and  is consistent with the value used by the EU Classification and Labelling Committee for soluble and sparingly soluble copper compounds.  This value is the lowest pH specific species mean acute value selected from 357 retained fish, algae and invertebrate and is referred to as the acute toxicity classification value.  A separate report with details on the acute toxicity classification value is attached for review (see See PRP ENV 05-60 , Van Sprang, 2005).

The observed acute ecotoxicity reference values for pH 7 and pH 8 media are respectively 47 and 30 µg Cu/L, based on measured ecotoxicity values.  A reference ecotoxicity value of 17.2 µg Cu/L (algae) was calculated at pH 8 using the BLM (See PRP ENV 05-60 , Van Sprang, 2005).    These ecotoxicity data will be used for comparison of the T/D data obtained at pH 7 & 8.

4a.- Surface area normalization to the diameter of a sphere

The detailed pH 6 data, summarized in annex I,  show surface area specific copper releases ranging from 0.64 to 2.22 µg Cu/mm2 . An average  surface release  of 1.15 µg Cu/mm2 is thus determined as typical  for massive copper covering a wide range of surface loadings.

As explained above, the Normalised Critical Surface Loadings (NCSL) of a 1 mm particle at 1, 10 and 100 mg/L cut off values can be calculated for copper as 0.67, 6.7 and 67  mm2/L, respectively.

The corresponding average Normalised Critical Value (NCV), being the copper releases of a 1 mm particle at 1, 10 and 100 mg/L loading, can than be calculated as respectively  0.77, 7.7 and 77 µg Cu/L (Table 1, and in detail in Annex I). Corresponding minimum and maximum NCV can be calculated using the minimum and maximum surface specific copper releases (see table 1, and Annex I).

The results of this normalization approach, as described in detail above, are presented below in Table 1.  Using this approach it was found that copper massives only at loadings greater than 100 mg/L are able to release enough ions to reach a concentration higher than the  L(E)C50 value (Table 1).  Therefore, the proposed acute classification is R52.

Table 1.- Comparison of acute toxicity classification value (29 µg/L) with the amount of copper in solution at the critical surface area, normalized to a 1 mm diameter sphere.

| CP, mg/L (loading) | NCSL, mm2/L | NCV, µg/L |
| --- | --- | --- |
|  |  | Average | Minimum | Maximum |
| 1 | 0.67 | 0.77 | 0.43 | 1.50 |
| 10 | 6.74 | 7.74 | 4.31 | 14.97 |
| 100 | 67.42 | 77.45 | 43.09 | 149.74 |
| Classification | CP, mg/L | Ratio NCV/E(L)C50 |  |
|  |  | Average | Minimum | Maximum |
| No classification | 1 | 0.03 | 0.01 | 0.05 |
| No classification | 10 | 0.26 | 0.14 | 0.50 |
| R52 | 100 | 2.58 | 1.44 | 4.99 |

CP = classification Cut off values based on loading; NCSL = normalized critical surface load;

NCV = normalized critical value.

Annex I also provides transformation/dissolution results obtained at pH 7 and 8  for copper wires tested at 100 mg/L loading rates.  These data allow to calculate the average amount of copper released from the copper massive surfaces at pH 7 and 8 :  0.190 and 0.127 µg Cu/mm2.  The resulting copper concentrations released after 7 days transformation/dissolution  of a 1 mm massive at pH 7 and 8  (Table 2) are below the  pH 7 & 8 acute reference values observed/calculated  (17-47 µg Cu/L).  The pH 7 & 8 data and therefore do thus not lead to a hazard classification and pH 6 data can be considered as a worst case scenario.

Table 2. - Determination of the amount of copper in solution from copper massives at different pHs.

| pH | NCSL, mm2/L at 100 mg/L | Average release | NCV at 100mg/L |
| --- | --- | --- | --- |
|  |  | µg Cu/mm2 | µg/L |
| 6 | 67.42 | 1.15 | 77.4 |
| 7 | 67.42 | 0.190 | 12.8 |
| 8 | 67.42 | 0.127 | 8.6 |

5.- Chronic hazard classification of copper massives

To assess the potential for chronic classification a T/D study was performed at pH 6.0 for  28 days with copper wires at a loading of  1 mg/L and a range of surface loadings (from 1.22 to 2.85 mm2/L).  In total, 4 assays were performed.

The chronic classification of copper massives was done using the approach for the acute classification, but using a CP of 1 mg/L and a T/D time of 28 days.  The results are summarized  in table 3 and the detailed results can be seen from Annex I

For purposes of assessing the T/D results, a chronic NOEC value of 24.5 ug/L  (12.8 µg Cu/L based on BLM modeled data) was derived from an extensive data base and used for Chronic  hazard classification.  The chronic data base derived for the voluntary copper risk assessment was utilized as a starting point and was evaluated to insure that all NOECs were for standard OECD species performed according to standard methods typically use for classification and labelling.  A separate report with details of this approach is attached for review (See PRP ENV 05-60 , Van Sprang, 2005).

Table 3.- Determination of the chronic classification of massive copper using loadings at 1 mg/L and a critical surface area approach.

| NCSL, mm2/L | NCV, µg/L |
| --- | --- |
|  | Average | Minimum | Maximum |
| 0.67 | 2.78 | 1.04 | 7.47 |
|  | Ratio NCV/E(L)C50 |
|  | Average | Minimum | Maximum |
|  | (2.78/24 =) 0.12 | (1.04/24 =) 0.04 | (7.47/24 = ) 0.31 |
|  | No classification as all values are less than 1.0 |

As demonstrated, it was found that copper massives at a loadings greater than 1 mg/L do not release enough ions to reach concentrations higher than the chronic NOEC value. Therefore a there is no need for chronic (R53) classification.

It is further worthwhile mentioning that the maximum surface specific release (11.1 µg Cu/mmm2) is extremely high compared to the other three chronic test results, ranging between 1.5 and 2.2 µg Cu/mm2. The maximum value is hence considered as an outlier.

No  28 days T/D was carried out with the 1 mg/L wires at the higher pHs  because the information on  acute hazard classification demonstrated that classification carried out at pH 6 represents a worst case scenario.

6. Conclusions

The data for massive copper, lead, under worst case conditions (pH6),  to an acute R52 classification with no need for chronic R53 classification.  Therefore, in accordance with the EU regulations, there is no need for classification of massive copper.

Annex I

1.- Dissolution transformation assays results

1a.- Results Acute Assays

|  | Wire diameter | Mass Loading | Specific Surface Area | Surface loading | Dissolved Copper | Dissolved Copper |
| --- | --- | --- | --- | --- | --- | --- |
|  | mm | mg/L | m2/g | mm2/L | 7 days, µg/L | 7 days, µg/mm2 |
| Acute 1 pH 6 | 0.16 | 100 | 2.809E-03 | 280.94 | 265.22 | 0.944 |
| Acute 2 pH 6 | 0.40 | 100 | 1.221E-03 | 122.15 | 83.41 | 0.683 |
| Acute 3 pH 6 | 0.98 | 100 | 4.737E-04 | 47.37 | 31.36 | 0.662 |
| Acute 4 pH 6 | 1.83 | 100 | 2.982E-04 | 29.82 | 19.06 | 0.639 |
| Acute 5 pH 6 | 0.16 | 1 | 2.809E-03 | 2.81 | 6.24 | 2.221 |
| Acute 6 pH 6 | 0.40 | 1 | 1.221E-03 | 1.22 | 2.13 | 1.744 |
|  |  |  |  |  | Average | 1.149 |
|  |  |  |  |  | Minimum | 0.639 |
|  |  |  |  |  | Maximum | 2.221 |
|  | Wire diameter | Mass Loading | Specific Surface Area | Surface loading | Dissolved Copper | Dissolved Copper |
|  | mm | mg/L | m2/g | mm2/L | 7 days, µg/L | 7 days, µg/mm2 |
| Acute 7 pH 7 | 0.16 | 100 | 2.809E-03 | 280.94 | 46.94 | 0.167 |
| Acute 8 pH 7 | 0.40 | 100 | 1.221E-03 | 122.15 | 18.17 | 0.161 |
| Acute 9 pH 7 | 0.98 | 100 | 4.737E-04 | 47.37 | 14.63 | 0.309 |
| Acute 10 pH 7 | 1.83 | 100 | 2.982E-04 | 29.82 | 3.68 | 0.124 |
| Acute 11 pH 8 | 0.16 | 100 | 2.809E-03 | 280.94 | 54.17 | 0.193 |
| Acute 12 pH 8 | 0.40 | 100 | 1.221E-03 | 122.15 | 13.86 | 0.123 |
| Acute 13 pH 8 | 0.98 | 100 | 4.737E-04 | 47.37 | 5.87 | 0.124 |
| Acute 14 pH 8 | 1.83 | 100 | 2.982E-04 | 29.82 | 2.28 | 0.076 |

1b.- Results Chronic Assays

|  | Wire diameter | Mass Loading | Specific Surface Area | Surface loading | Dissolved Copper | Dissolved Copper |
| --- | --- | --- | --- | --- | --- | --- |
|  | mm | mg/L | m2/g | mm2/L | 28 days, µg/L | 28 days, µg/mm2 |
| Chronic 1 | 0.16 | 1.00 | 2.84E-03 | 2.84 | 35.14 | 11.08 |
| Chronic 2 | 0.40 | 1.00 | 1.22E-03 | 1.22 | 7.19 | 2.29 |
| Chronic 3 | 0.16 | 0.43 | 2.84E-03 | 1.23 | 5.40 | 1.55 |
| Chronic 4 | 0.40 | 1.00 | 1.22E-03 | 1.22 | 5.15 | 1.55 |
|  |  |  |  |  | Average | 4.118 |
|  |  |  |  |  | Minimum | 1.547 |
|  |  |  |  |  | Maximum | 11.082 |

Annex II

Procedures

EQUIPMENT AND INSTRUMENTS

Test vessels:

2.0 liter Erlenmeyer Flask made by Ilmabor, Germany.

Agitation method:

Orbital shaker:

·	Custom made top loading orbital shakers with a 2.54 cm orbit (Fig 1). They can hold 3 liter flasks inside an enclosed environment, allowing control of the test solution pH through control of its atmospheric CO2 pressure.

·	These shakers were built with a gas intake to inject gas from the CO2 cylinders into the shaker’s enclosed atmosphere, where the test flasks are agitated. The shakers also have an exhaust vent where the gas flows out.

·	Test temperature is controlled through control of the laboratory’s temperature, within 2°C

·	Test vessel:  2 litre Erlenmeyer flasks, made by Ilmabor, Germany

·	The tests have been conducted at normal room light conditions.

Figure 1

pH meter:

Fisher Scientific Accumet model 25, with temperature measuring capability and automatic temperature correction. Resolution: 0.1 pH units, accuracy +/- 0.002.

Centrifuge:

No centrifuge has been used in these tests. All sample solutions are filtrated.

Scales:

Chyo 180-J (for 100 mg/L loading), calibrated before each set of measurements. Readability:  0.1 mg. For loading of 1 and 10 mg/L a Sartotius MC-5 scale was used, keep in a room at constant temperature and humidity, readability 1 microgram.

Dissolved oxygen (D.O.) meter:

Orion Dissolved oxygen meter Model 97-08 with temperature measuring capability and automatic temperature correction. Range: 0.0 to 14.0 mg/l; resolution +/- 0.05 mg/l. Resolution:  0.05 mg/l; relative accuracy ±2% full scale; temperature range: 0 to 45°C; temperature resolution:  0.1°C; temperature accuracy ± 1

Sample tubes:

120 mm  x 15 mm conical polypropylene tubes, 14 ml capacity

Gas handling and control equipment:

Custom built for our laboratory, including CO2 cylinders and handling equipment to drive the gas through the shaker’s enclosed atmosphere. No CO2 is injected directly into the flasks. Instead, the solution’s pH is controlled by controlling the CO2 pressure inside the shaker, where the test flasks are agitated. The system includes:

·	One Harris model 825 CO2 regulator connected to each cylinder.

·	Electric heaters over the regulators´ output to avoid freezing of the gas.

·	Gas flow control valves between the regulators and the flow meters.

·	One AGA model 3805 flow meters for each cylinder, connected to each flow control valve.

·	Another flow meter before the shaker’s intake.

·	The gas goes into the shaker through a gas intake, where it mixes with atmospheric air.

·	The mixed gas circulates through the enclosed atmosphere where the test flasks are hold, and goes out through an exhaust vent.

·	Sample solution pH is monitored continuously during the tests

Volumetric labware:

·	10 and 5 l Schott Geratte glass bottles, for media preparation.

·	Boeco Germany Micropipettes, with polypropylene tips:

·	1000 a 5000 μl  10 μl at 22C.

·	200 a 1000 μl  2 μl at 22C.

·	50 a 200 μl  0.8 μl at 22C.

·	Volumetric flasks:

·	3000.00 ml   0.50 ml glass flasks, made by Ilmabor, Germany

·	2000.00 ml   0.50 ml  Pyrex TC 20C no. 5642;

·	1000.00 ml   0.30 ml Pyrex TC(IN)20C no.5642;

·	100.00 ml   0.10 ml glass, Schott Duran A (IN)20C no. 9801

Filtration:

For aqueous media:

0.2 μm pore size Gelma Sciences filter, or equivalent, in a water aspiration configuration, driven by two Cole Palmer Masterflex peristaltic pumps.

for filtration of samples:

13 mm diameter, 0.2 μm pore size membrane filter, on a reusable Millipore Syringe.

REAGENTS

Water Purification System:

Whenever referring to “d.i. water” throughout the present report, it is referring to 18 M resistance water produced by a Millipore Super-Q Water Purification system comprising:

·	a Millipore ion exchanger resin system

·	a Millipore Polygard Particles filter unit;

·	a Millipore Carbon filter unit;

·	a Millipore ROPAK module, reverse osmosis and electro ionization system;

Millipore Super-Q system comprising:

·	a Millipore Super C (Organic matter) filter unit;

·	2 Millipore Ion-Ex  (Inorganic matter) filter unit and

·	Millipore Durapore TP de 0.22) filter (for micro organisms and particles larger than 0.22 μm)

The system is capable of produce water with less that 1 µg/L of totals metals and 0.05 mg/L of  total organic carbon.

Gases:

F grade CO2 from Indura Company, according to Chilean regulation N°2179, with 99.5% minimum purity; maximum impurities as following (in ppm):  H2S 1, NO2 5, SO2 5, NH3 2.5, H2O 60.

Aqueous media and pH

The stock OECD 203 test medium was prepared by diluting the required amounts of reagents All the chemicals were purchased from Merck (Germany) unless is stated, and were of Pro Analysis quality or better., according to the target pH desired, in 10 liters of Q-water. The amounts of each reagent are selected according to the data in Table I.

·	Each of the required reagents is weighted on a weighting paper.

·	The required amount for the desired pH is dissolved in 10 liters of deionised water, in a 10 liter bottle fitted with a magnetic stirring bar (Teflon coated),

·	The solution is stirred for one hour, or more if necessary to homogenize.

·	The solution obtained is then filtered with a 47 mm diameter, 0.2 μm pore size cellulose acetate filter.

On the resulting solution the pH was measured.

Before each test, the medium was agitated until O2 concentration and temperature are balanced. During the tests, pH is stabilized around the desired value using CO2 injected into the shaker, when necessary.

Sample solution pH is monitored continuously during the tests

Table I.-

| TARGET PH : 8 |
| --- |
| Reagent | Target dilution (mg/L) | Reagent required for 10 liters (mg) | Purity of reagent % | Amount of reagent to be weighted (g) |
| NaHCO3 | 65.7 | 657 | 99.7 | 0.6590 |
| KCl | 5.75 | 57.5 | 99.8 | 0.0578 |
| MgSO4 *7H2O | 123 | 1230 | 99.5 | 1.2362 |
| CaCl2*2H2O | 294 | 2940 | 99.5 | 2.9548 |

Solutions for pH 6.0 were prepared by a 10 fold dilution of the stock pH 8.0 solution

General:

Cleaning of flasks, carboys and bottles is done:

·	soaking  for 12 hours with 2% Extran detergent

·	Rinsing with abundant d.i. water (Q-water) until all soap has been eliminated

·	Soaking 12 hours in a 10% HNO3 solution

·	Rinse again with d.i. water

·	Soaking in a 10% HCL in d.i. solution for 12 hours

·	Rinse again in d.i. water

·	Once dry, store covered with Parafilm.

Cleaning of syringes, 14 ml tubes and sample tube tops: These are clean when purchased, and disposed after being used.

Chemical analyses:

Analytical instrumentation:

Perkin Elmer Elan 6100 ICP-MS (inductively coupled plasma-mass spectrometer) for Cu, Co and Ni determinations

Perkin Elmer AAnalist 800 graphite furnace with Zeeman Correction GF-AAS (graphite furnace-atomic absorption spectrophotometer) used for Fe determinations.

The determinations were carried out following the Environmental Protection Agency (USA) methods 200.8 Trace Elements by ICP/Mass Spectrometry. Methods for the Determination of Metals in Environmental Samples Supplement 1 (EPA/600/R-94/111) rev. 5.4 for ICP-MS and 200.9 Trace Elements by Stabilized Temperature Graphite Furnace AA Spectrometry. Methods for the Determination of Metals in Environmental Samples Supplement 1 (EPA/600/R-94/111) rev. 2.2 for GF-AAS

Detection Limits

|  | Copper |
| --- | --- |
| Limit of Detection, µg/L | 0.030 |

Detection limits for Cu in ICP-MS

Quality assurance solutions:

Standard solutions were as follows:

·	QCS-26 was obtained from High Purity Co., Charleston, South Caroline, USA.

·	TMDA-62 reference material was purchased from the National Research Institute, Canada.

Each of the standards were diluted in the proper matrix (Media OECD 203 for the target pH)

Tests procedures

The test were conducted using the SOP distributed by the OECDThe Standard Operating Procedure for the Transformation/Dissolution of Metals and Sparingly Soluble Metal Compounds, Version February 2004.   and following as close as possible the GLP guidelines proposed by OECD OECD Principles on Good Laboratory Practice (as revised in 1997), ENV/MC/CHEM(98)17.